## Slide 1: MBW-MQW
Some initial considerations on expected life and available options
Presented by P. Fessia
Fluka analysis: Francesco Cerutti, Anton Lechner, Eleftherios Skordis
Collimation input: Rodrick Bruce, Stefano Redaelli , Belen Maria Salvachua Ferrando
MNC team: Paolo Fessia, Pierre Alexandre Thonet, D. Tommasini
Power Converter: Hugues Thiesen
Optics: Massimo Giovannozzi
MME design office: L. Favre, T. Sahner
Analysis of Epoxy resins: E. Fornasiere (TE-MSC-MDT)

## Slide 2: The problem / the magnets
Due the expected difference in losses between point 7 and point 3 we concentrate here on point 7 (after TS 2012 factor 10 less before factor 3)

## Slide 3: MQW
characteristics | RQ4.LR7 | RQ5.LR7 | RQT4.L7 | RQT5.L7 | RQT4.R7 | RQT5.R7 | RQ4.LR3 | RQ5.LR3 | RQT4.L3 | RQT5.L3 | RQT4.R3 | RQT5.R3
I ultimate (from layout database) [A] | 810 | 810 | 600 | 600 | 600 | 600 | 810 | 810 | 600 | 600 | 600 | 600
Voltage I ultimate [V] | 381 | 383 | 29 | 31 | 27 | 29 | 451 | 452 | 38 | 34 | 42 | 39
I 7 TeV (Fidel report) [A] | 598 | 610 | 151 | 17 | 151 | 17 | 561 | 593 | 313 | 441 | 313 | 441
Voltage I 7 TeV [V] | 282 | 289 | 8 | 2 | 8 | 2 | 313 | 331 | 20 | 31 | 22 | 29
Number magnet in series in circuit | 10 | 10 | 1 | 1 | 1 | 1 | 10 | 10 | 1 | 1 | 1 | 1
Turn/magnet | 171 |  |  |  |  |  |  |  |  |  |  | 
Estimated ultimate inter-turn voltage [V] | 0.22 | 0.22 | 0.17 | 0.18 | 0.16 | 0.17 | 0.26 | 0.26 | 0.22 | 0.2 | 0.25 | 0.23
Estimated inter-turn voltage at 7 TeV [V] | 0.16 | 0.17 | 0.05 | 0.01 | 0.05 | 0.01 | 0.18 | 0.19 | 0.12 | 0.18 | 0.13 | 0.17
Estimated inter layer voltage | Same as inter turn |  |  |  |  |  |  |  |  |  |  | 
Insulation thickness inter turn | 2X(2X0.25) mm=1 mm glass tape |  |  |  |  |  |  |  |  |  |  | 
Circuit energy ultimate [Kj] | 154 | 164 | 9 | 9 | 9 | 9 | 154 | 164 | 9 | 9 | 9 | 9
Circuit energy 7 TeV [Kj] | 84 | 93 | 0.6 | 0.01 | 0.6 | 0.01 | 74 | 88 | 2.5 | 5 | 2.5 | 5
Ground insulation | 1X(2X0.25) mm+3X(2X0.25)=2 mm |  |  |  |  |  |  |  |  |  |  | 
Resin used | EPN1138 42%+ GY 6004 42% + CY 221 16% + HY 905 100 %+ 30ml DY 073 |  |  |  |  |  |  |  |  |  |  | 
Dielectric resin | > 20 kV/mm |  |  |  |  |  |  |  |  |  |  | 

## Slide 4: MBW
characteristics | RD34.LR7 | RD34.LR3
I ultimate [A] (layout database) | 810 | 810
Voltage I ultimate [V] | 440 | 700
I 7 TeV (Fidel report) | 643 | 643
Voltage I 7 TeV | 350 | 556
Number magnet in series in circuit | 8 | 12
Turn/magnet | 84 | 
Estimated ultimate inter-turn voltage [V] | 0.65 | 0.7
Estimated inter-turn voltage 7 TeV [V] | 0.52 | 0.55
Estimated ultimate inter layer voltage [V] | 9.2 | 9.7
Estimated inter layer voltage 7 TeV [V] | 7.2 | 7.8
Circuit energy ultimate [Kj] | 472 | 793
Circuit energy 7 TeV [Kj] | 297 | 500
Insulation inter turn [mm] | 2X(2X0.15)=0.6 glass tape | 
Insulation inter layer [mm] | 2X(2X0.15)+2X(2X0.15)+1(glass cloth) =1.6 glass tape | 
Ground insulation | 2X(2X0.15)+1.5(0.15Xx)=1.8 | 
Resin used | EPC-1: resin ED-16 100 Hardener MA 2.28  K Plasticizer MGF-9 20 TEa accelerant 0.5 | 
Dielectric resin | ? (>>15kV/mm) | 

## Slide 6: Do they survive till LS2 (100 fb-1 >150 fb-1) do they survive till LS3 (300 fb-1 >350 fb-1) Do they survive till …
The questions

## Slide 7: MQWA.E5R7 Dose 2d cross section at maximum
Dose (MGy)
Normalization: 1.15 1016 p (30-50 fb-1 ).
Computations with E 6.5 TeV relaxed collimator settings

## Slide 8: MQWA.E5R7 Dose 2d cross section at maximum
Normalization: 1.15 1016 p (30-50 fb-1 ).
Computations with E 6.5 TeV relaxed collimator settings

## Slide 9: MQWA.E5R7 Dose Maximum Z profile
Beam 2
1.85 MGy
Normalization: 1.15 1016 p (30-50 fb-1 ).
Computations with E 6.5 TeV relaxed collimator settings

## Slide 10: MQWA.D5R7 Dose Maximum Z profile
Beam 2
0.8 MGy
0.8/1.85=0.4
Normalization: 1.15 1016 p (30-50 fb-1 ).
Computations with E 6.5 TeV relaxed collimator settings

## Slide 11: Ratio of total load on left Horizontal coils of magnets
Beam 2
MBW.B
MBW.A
TCAP
MQWA.E5R7
MQWA.D5R7
Values are in percentage (%)
Values normalized to most impacted one (MQWA.E5R7) : 12.6 GeV/p
3
4
5
14
11
29
17
19
21
27
34
100

## Slide 12
Magnet | Fluka estimation 50 fb-1 old loss pattern [MGy] | Fluka ratio peak to peak [%] | Fluka ratio total load [%] | Fluka ratio peak to peak normalised second magnet [%] | Fluka ratio total load normalised second magnet [%] | Extrapolated values old loss pattern [Mgy] | Reference extrapolation 50 fb-1 new loss pattern [MGy]
MQWA.A4 |  |  | 3 % |  | 9% | 0.08 | 0.2
MQWA.B4 |  |  | 4 % |  | 12% | 0.11 | 0.2
MQWA.C4 |  |  | 5 % |  | 15% | 0.14 | 0.3
MQWB.4 |  |  | 14 % |  | 41% | 0.37 | 0.8
MQWA.D4 |  |  | 11 % |  | 32% | 0.29 | 0.6
MQWA.E4 |  |  | 29 % |  | 85% | 0.77 | 1.6
MQWA.A5 | 0.39 | 21 % | 17 % | 43% | 50% |  | 0.8
MQWA.B5 | 0.52 | 28 % | 19 % | 57% | 56% |  | 1.1
MQWA.C5 | 0.61 | 33 % | 21 % | 68% | 62% |  | 1.3
MQWB.5 | 0.73 | 40 % | 27 % | 82% | 79% |  | 1.6
MQWA.D5 | 0.9 | 49 % | 34 % | 100% | 100% |  | 1.9
MQWA.E5 | 1.85 | 100 % | 100 % | 206% | 294% |  | 4.0

## Slide 13: MBWB Dose 2d cross section at maximum
Dose (MGy)
Normalization: 1.15 1016 p (30-50 fb-1 )

## Slide 14: MBWB Dose 2d cross section at maximum
Dose (MGy)
Normalization: 1.15 1016 p (30-50 fb-1 )

## Slide 15: MBWA - MBWB Dose Maximum Z profile
Beam 2
MBW.B
MBW.A
TCAP
MQWA.E5R7
MQWA.D5R7
MBW.A6R7
MBW.B6R7
Beam 2
Beam 2
Normalization: 1.15 1016 p (30-50 fb-1 )
MBW.B6R7-> 3 MGy/ 50fb-1
MBW.A6R7->2.5 MGy/ 50fb-1
Weighted on energy
MBW.B6R7-> 6 MGy/ 50fb-1
MBW.A6R7->5 MGy/ 50fb-1

## Slide 16: Future scenarios
magnet | Reference extrapolation 50 fb-1 new loss pattern [Mgy] | Till LS2 7TeV (150 fb-1) [MGy] | Till LS3 7TeV (350 fb-1) [MGy] | Till HL-LHC 7TeV (3000 fb-1) [MGy]
MBW.B6R7 | 5 | 16 | 38 | 323
MBW.A6R7 | 6 | 20 | 45 | 388
MQWA.A4 | 0.12 | 0.6 | 1.4 | 12
MQWA.B4 | 0.14 | 0.6 | 1.4 | 12
MQWB.4 | 0.18 | 0.9 | 2.1 | 18
MQWA.C4 | 0.52 | 2.4 | 5.6 | 48
MQWA.D4 | 0.4 | 1.8 | 4.2 | 36
MQWA.E4 | 1.1 | 4.8 | 11 | 96
MQWA.A5 | 0.62 | 2.4 | 5.6 | 48
MQWA.B5 | 0.7 | 3.3 | 7.7 | 66
MQWB.5 | 0.8 | 3.9 | 9.1 | 78
MQWA.C5 | 1 | 4.8 | 11 | 96
MQWA.D5 | 1.3 | 5.7 | 13 | 114
MQWA.E5 | 3.7 | 12 | 28 | 240

## Slide 17
Life evaluation
Resin radiation resistance
Screening
Alternative operation schemes

## Slide 18: Radiation resistance

## Slide 19: MQW resins
Resin used |  |  |  |  | 
component | EPN1138 | GY 6004 | CY 221 | HY 905 | 30ml DY 073
percentage | 50 % | 50 % | 20 % | 120 % | 0.03
EPN 1138 | Novolac
GY 6004 | DGEBA
CY 221 | DGEBA
HY 905 | HPA
DY 073 | flexibilizer

## Slide 21: Different epoxy
Resins |  | Hardeners | Additives | Composition (p.p.) | Mix Temp (°C) | Viscosity (cPs) | Service life (mn) | Fig | Dose for 50% flex. (MGy) | Dose Range (MGy)
EDBAH |  | MA |  |  |  |  |  | 5.4 | 1.4 | 1 - 3
EDBAH |  | MA | BDMA | 100-105-0.2 | 80 | 45 | >180 | 5.1 | 1.6 | 
BECP |  | MA |  |  |  |  |  | 5.4 | 2.5 | 
BECP |  | MA | BDMA | 100-110-0.2 | 80 | 40 | >180 | 5.1 | 2.3 | 
ECC |  | MA |  | 100-72 | 80 | 20 | >240 | 5.5 | 1.8 | 1 - 6
VCD |  | MA | BDMA | 100-160-05 | 60 | 20 | >180 | 5.4 | 3.7 | 
DADD |  | MA |  | 100-65 | 80 | 180 | >240 | 5.4 | 5.5 | 
DGEBA + | EDGDP | TETA |  | 100-20-12 | 25 |  |  | 5.21 | 1.3 | 1 - 2
DGEBA |  | TETA | DBP | 83-9-17 | 50 | 500 | few | 5.22 | 1.2 | 
DGEBA |  | DADPS |  | 100-35 | 130 | 60 | 180 | 4.2 | 5.1 | 5 - 15
DGEBA + | EDGDP | MDA |  | 100-20-30 | 80 |  |  | 5.21 | 8.2 | 
DGEBA |  | MDA |  | 100-27 | 80 | 100 | 50 | 5.9 | 13.0 | 
DGEBA |  | MPDA |  | 100-14.5 | 65 | 200 | 30 | 5.7 | 23.5 | 23
DGEBA |  | AF |  | 100-40 | 100 | 150 | 30 | 5.26 | 45.2 | 45
DGEBA |  | DDSA | BDMA | 100-130-1 | 80 | 70 | 120 | 5.2 | 4.2 | 5 - 15
DGEBA |  | NMA | BDMA | 100-80-1 | 80 | 80 | 120 | 5.2 | 5.9 | 
DGEBA |  | MA |  | 100-100 | 60 | 69 | >1440 | 5.23 | 7.1 | 
DGEBA |  | MA | BDMA |  |  |  |  | 5.1 | 12.0 | 
DGEBA |  | MA | BDMA + Po. Gl. | 100-100-0.1-10 | 60 | 65 | 300 | 5.23 | 12.1 | 
DGEBA |  | AP |  | 100-70 | 120 | 26 | 180 | 5.2 | 13.0 | 
DGPP |  | DADPS |  | 100-28 | 130 |  |  | 5.6 | 8.2 | 5 - 15
DGPP |  | MA |  | 100-135 | 120 |  |  | 5.3 | 13.0 | 
EDTC |  | MDA |  | 100-20 | 80 |  | 40 | 5.9 | 10.0 | 
TGTPE |  | DADPS |  | 100-34 | 125 | >20000 |  | 5.6 | 12.1 | 
TGTPE |  | MA | BDMA | 100-100-0.2 | 125 | >15000 |  | 5.3 | 10.6 | 
EPN |  | DADPS |  | 100-35 | 100 |  | 30 | 5.6 | 23.5 | 20 - 40
EPN |  | MDA |  | 100-29 | 100 |  | 35 | 5.10 | 37.2 | 
EPN |  | HPA | BDMA | 100-76-1 | 80 |  | 40 | 5.10 | 13.0 | 10 - 20
EPN |  | MA | BDMA | 100-105-0.5 | 80 |  | 100 | 5.3+5.25 | 15.0 | 
EPN |  | NMA | BDMA | 100-85-1 | 100 |  | 80 | 5.10 | 20.6 | 
TGMD |  | DADPS |  | 100-40 | 80 |  | 50 | 5.6 | 20.6 | 10 - 25
TGMD |  | MA | BDMA | 100-136-0.5 | 60 |  | 30 | 5.3 | 11.4 | 
TGMD |  | NMA | BDMA | 100-110-1 | 80 | 500 | 20 | 5.8 | 18.0 | 
TGPAP |  | NMA |  | 100-137 | 80 | <20 |  | 5.8 | 23.5 | 
DGA |  | MPDA |  | 100-20 | 25 |  | 120-420 | 5.7 | 23.5 | 20 - 30
DGA |  | NMA |  | 100-115 | 25 | 5 - 20 | 30-5760 | 5.8 | 28.6 | 
Legend | 
Resin | 
 | Linear aliphatic
 | Cycloaliphatic
 | Aromatic
Hardener | 
 | Aliphatic Amine
 | Aromatic Amine
 | Alicyclic Anhydride
 | Aromatic Anhydride
Aromatic > Cycloaliphatic > Linear Aliphatic
Aliphatic amine harderner  poor radio-resistance
Aromatic amine hardener >
Anhydride hardener
H: Too high local concentration of benzene may induce steric hindrance disturbation
Good radio-resistance even if Cl (tendence to capture nth)
Novolac: HIGH Radio-resistance
Large nb of epoxy groups  Density + rigidity
Glycidyl-amine: HIGH R.-resistance
Quaternary carbon  weakness
Ether group (R – O – R’)  weakness
 Repl. by amina

## Slide 22: DGEBA MY 745 substituted by GY 6004

## Slide 23: CY 222 (similar to CY 221)

## Slide 25: MBW BINP used resin. We looked at molecule and there is good indication that it should radiation hard as witnessed by the tests

## Slide 26: 1st conclusion
MQW
- The pure resin mix used shall keep substantial mechanical properties at least till 15-20 MGy
MBW
- The pure resin mix used shall keep substantial mechanical properties at least till 40-50 MGy

## Slide 27: Filler contribution
Resins | Hardeners | Additives | Filler | Composition (p.p.) | Fig | Dose for 50% flex. (MGy) | Dose Range (MGy)
DGEBA | MDA |  | Papier | 100-27-200 | 5.14 | 1.3 | 1 - 2
DGEBA | MDA |  | Silice | 100-27-200 | 5.14 | 10 | 10 - 15
DGEBA | MDA |  | Silice | 100-27-200 | 5.18 | 11.4 | 
DGEBA | MDA |  | Silice (5 micron) | 100-27-20 | 5.16 | 14.8 | 
DGEBA | MDA |  | Silice (20 micron) | 100-27-20 | 5.16 | 14.8 | 
DGEBA | MDA |  | Silice (40 micron) | 100-27-20 | 5.16 | 14.6 | 
DGEBA | MDA |  | Silice (40 micron) | 100-27-200 | 5.17 | 12.1 | 
DGEBA | HPA | BDMA | Silice (40 micron) | 100-80-2-200 | 5.17 | <10 | <10
DGEBA | MDA |  | Aérosil + Sulphate de Barium | 100-27-2-150 | 5.14 | 15.8 | 15
DGEBA | MDA |  | Magnésie | 100-27-120 | 5.14 | 18 | 18
DGEBA | MDA |  | Graphite | 100-27-60 | 4.6 | 26.8 | 25 - 30
DGEBA | MDA |  | Graphite | 100-27-60 | 5.14 | 30.5 | 
(DGEBA | MDA |  | Alumine | 100-27-220 | 4.7 | 23.5) | 20 - 50
DGEBA | MDA |  | Alumine | 100-27-220 | 5.14 | 51.7 | 
DGEBA | MDA |  | Alumine | 100-27-100 | 5.15 | 20.6 | 
DGEBA | MDA |  | Alumine | 100-27-220 | 5.15 | 42.5 | 
DGEBA | MDA |  | Fibre de verre | 100-27-50 | 5.19 | 82 | 80 - 100
DGEBA | MDA |  | Fibre de verre | 100-27-60 | 5.18 | 100 | 
EPN | MDA |  | Fibre de verre | 100-29-50 | 5.19 | >100 | >100
TGMD | MDA |  | Fibre de silice | 100-41-50 | 5.20 | >100 | >100
TGMD | DADPS |  | Fibre de silice | 100-40-50 | 5.20 | >100 | 
Legend | 
Resin | 
 | Linear aliphatic
 | Cycloaliphatic
 | Aromatic
Hardener | 
 | Aliphatic Amine
 | Aromatic Amine
 | Alicyclic Anhydride
 | Aromatic Anhydride
Paper [cellulose (C6H10O5)n]
 Strong decrease of radio-resistance
2 Categories of fillers:
Powder fillers
Glass/Silice fibers
The bigger the powder, the more radio-resistant
Hardener choice not influenced by filler
High r.-resistance for Graphite and Alumina
The more fillers, the more radio-resistant
Best Radio-Resistant materials are obtain with Glass/Silice (influence of boron) fibers and aromatic resins (Novolac and glycidyl-amine)

## Slide 28
fibre

## Slide 29
fibre

## Slide 30: 2nd conclusion
MQW
- Presence of glass fibre shall increase the substantial mechanical properties at least to 30-40 MGy
MBW
- Presence of fibre glass should probably extend life till 60- 70 MGy

## Slide 31: Caveat
We need to perform a rough evaluation of stresses to demonstrate that we are effectively in a low stress situation

## Slide 32: Screens

## Slide 33: Screen options
 | MQW | MBW
where | Between iron poles and the coil | Between coil ends and vacuum chamber
Possible thickness | 15-30 mm | 2-4 mm
Segmentation | Yes for easy extraction and possibility to tune material along the length | no
Materials | Tungsten/steel | Tungsten

## Slide 34: Looking for screen efficiency of …
magnet | Till LS3 7TeV (350 fb-1) [MGy] | Factor to gain | Till HL-LHC 7TeV (3000 fb-1) [MGy] | Factor to gain
MBW.B6R7 | 38 | Not necessary but good for ageing | 323 | 6
MBW.A6R7 | 45 | Not necessary but good for ageing | 388 | 7
MQWA.A4 | 1.4 |  | 12 | 
MQWA.B4 | 1.4 |  | 12 | 
MQWB.4 | 2.1 |  | 18 | 
MQWA.C4 | 5.6 |  | 48 | 1.5
MQWA.D4 | 4.2 |  | 36 | 
MQWA.E4 | 11 |  | 96 | 3
MQWA.A5 | 5.6 |  | 48 | 1.5
MQWA.B5 | 7.7 |  | 66 | 2
MQWB.5 | 9.1 |  | 78 | 2.5
MQWA.C5 | 11 |  | 96 | 3
MQWA.D5 | 13 |  | 114 | 3.5
MQWA.E5 | 28 | (1.5) | 240 | 7

## Slide 35: MQWA.C5R7 Dose Maximum Z profile
Normalization: 1.15 1016 p (30-50 fb-1 )
Beam 2
0.73 MGy
0.3 MGy
We need factor 3
We need factor 2

## Slide 36: MQW screen fast prototyping pieces to be produced on Monday. Then test of insertion with the vacuum chamber and geometry to FLUKA team MBW under design

## Slide 37: The different operating scenarios

## Slide 38: Different scenarios see slides from M. Giovannozzi
Other operating scenarios
Option A
Reconfigure the MQWA in pos. C5 as MQWB
Remove MQWA.E5
Connect new MQWB.C5 in the circuit RQ5.LR7
Substitute MQWA.E5 with an absorber at least effective as previous MQWA.E5
Option B
Connect MQWA.E5 on a new power supply circuit (600 A)
In case of failure of MQWA.E5 ramp up the other 4 magnets to 810 A to regain the previous strength
Not applicable because of saturation and b3 increase

## Slide 39: Conclusions
LS2 shall be reached by both MQW and MBW
LS3 should be reached by both MQW and MBW, but MQWA.E5 and MBW. X6 will have accumulated some ageing dose. Run (resins test in parallel with representative geometry to confirm)
In HL-LHC perspective
  MQW could meet the target combining screening and modified operation scenario
  MBWs need a very effective screen. Due to the available space looks to be a challenge
We should try to install screens in MQWA. E5 and MQWA.D5 and MBW already in LS1 to prevent ageing
In LS2 we should target to implement the new operation scenario
Probable need to design and build a new MBW for LS3 (HL-LHC operation)

## Slide 40
LHC Point 7
Ambient dose equivalent rates in µSv/h at 40cm
measured on Dec 20, 2012
(last “good” fill on Dec 5, i.e. cooling time >1week)
tcool | Scaling factor
One hour | 1.4
One day | 1.0
One week | 0.73
One month | 0.45
4 months | 0.20
Scaling factors
based on generic
Studies for IR7:

## Slide 41: appendix

## Slide 42
If we put the 2 MQWA.E on 2 separate power converters 600 A …

## Slide 43: History (SPS, ISR, …)

## Slide 45
ISR~MQW
SPS

## Slide 49: Electrical Properties Changes 2
Volumetric Resistivity r (Ω·cm)
1010
1011
1012
1013
1014
1015
1016
1017
0
20
40
60
80 100 120 140 160 180 200 Temp. (°C)
○ DGEBA + MDA
x EPN + MDA
∆ TGMD +MDA
_______ Non irradié
_ _ _ _ _ 2.7x109 rad
T ↑ => r ↓
r = ~1016 Ω·cm @RT
High mechanical radio-resistance  High electrical resistance (mechanical degradation occurs first)
Example of low mechanical-resistance system:
DGEBA-DBP-TETA  r = ~1013 Ω·cm @RT for 6.8x108 rad

## Slide 50: DGEBA considerations

## Slide 51: PROPOSALS I
 | Traction test | Flexural test | Leakage current in air humid | Dielectric in air humid | Leakage current in air humid after 1 month in water | Dielectric in air humid after 1 month in water
0 MGy | Y | Y | (Y) | Y | (Y) | Y
10 Mgy |  | Y | (Y) | Y | (Y) | Y
20 Mgy | Y | Y | (Y) | Y | (Y) | Y
40 Mgy | Y | Y | (Y) | Y | (Y) | Y
50 MGy |  |  | (Y) | Y | (Y) | Y
60 MGy | Y | Y | (Y) | Y | (Y) | Y
70 MGy | Y | Y | (Y) | Y | (Y) | Y
Wafer 1 and 2 mm thickness resin and glass fibre

## Slide 52: PROPOSALS II
 | Shear test | Leakage current in air humid | Dielectric in air humid | Leakage current in air humid after 1 month in water | Dielectric in air humid after 1 month in water
0 MGy | Y | (Y) | Y | (Y) | Y
10 Mgy |  | (Y) | Y | (Y) | Y
20 Mgy | Y | (Y) | Y | (Y) | Y
40 Mgy | Y | (Y) | Y | (Y) | Y
50 MGy |  | (Y) | Y | (Y) | Y
60 MGy | Y | (Y) | Y | (Y) | Y
70 MGy | Y | (Y) | Y | (Y) | Y
Insulated cables, 2 resins, 3 samples